## Slide 1
Partner name
Spray Coating
KDFs – to be determined
Process
Characterisation / Functionality test
Product
Legend
Input/output
Case Study 2 – Water Membranes
Precursors
Solution Combustion Synthesis
Characterisation
XRD, XPS, N2 adsorption measurements, temperature programmed reductions, SEM, TEM.
Synthesis Steps
Dip Coating from combustion sol
Sonochemical coating
Incorporation Step – SiC scraps
Coated SiC 1
Coated SiC 2
Coated SiC 3
Spray Coating
Dip Coating from combustion sol
Sonochemical coating
Coated SiC 4
Coated SiC 5
Coated SiC 6
Spray Coating
Dip Coating from combustion sol
Sonochemical coating
Coated SiC 7
Coated SiC 8
Coated SiC 9
SEM, TEM
Functionality tests
Antibacterial properties
SiC scraps - thermocatalytic properties
Mechanical tests
Stability in water (leaching)
CSF-Sil1-Rust
CSF-Sil1-Rice
CSF-Sil1-Rust-Rice
Ce-doped SrFeO3_SiO2 NMs
Bio-SiO2@TiO2
NPs
bio-SiO2
Solution TiO2 hydrothermal coating
Spray Coating
Sonochemical coating
Coated SiC 10
Coated SiC 11
Incorporation Step –SiC flat membranes
Stage Gate
Best NPs
selected for
incorporation
TPBR SiC 1
TPBR SiC 2
TPBR SiC 3
TPBR SiC 4
TPBR SiC 5
TPBR SiC 6
TPBR SiC 7
TPBR SiC 8
TPBR SiC 9
TPBR units
from SiC scraps
MF SiC 10
MF SiC 11
Micro Filtration units
from SiC flat membranes
TEM, SEM, TGA, XPS, antibacterial activity, leaching (water)
Functionality tests
Water quality (leaching, BPA residuals, bacteria)
Functionality tests
Water quality (leaching, BPA residuals, bacteria)
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
TPBR incorporation
Micro Filtration Unit incorporation
Micro Filtration Unit incorporation
KDFs - CSF-SIL1 synthesis
Silica from rice husk; rust waste; both.
Synthesis – reducer to oxidiser ratio (continuous, 1-1) or pH (continuous variable range 2-7).
KDFs - Bio-SiO2@TiO2 synthesis
Ratio of titania precursor to ethanol.
Temperature (°C)/time (h) of the hydrothermal synthesis.
KDFs – Dip-coating of CSF-SIL1
Sol concentration (g/L)
Number of subsequent coatings/coating time (min)
KDFs – Sonochemical coating of CSF-SIL1
Initial concentration of the nanoparticles/reaction time.
KDFs – Spray coating of CSF-SIL1
Flow rate/belt speed
Nanoparticle concentration in the dispersion (mg/L)
KDFs – Spray coating of bio-SiO2@TiO2
Screening to decide between: flow rate (ml/min), belt speed (m/min), nanoparticle concentration.
KDFs – Sonochemical coating of bio-SiO2@TiO2
Initial concentration of the nanoparticles/reaction time.
Do you expect the reductant:oxidant ratio to have a broadly similar impact on the KPIs for each of the three CSF-Sil1 types? If so, reductant:oxidant ratio experiments could be conducted with just one of the CSF-SIL1 types, and the optimum conditions applied to the synthesis of the three types.
Temp and time are two distinct KDFs. Will you choose just one of these KDFs to examine?
No. of coatings and coating time are two distinct KDFs but could result in similar impact on KPIs. Will you choose just one of these?
Flow rate and belt speed are two distinct KDFs but their combinations can result in similar levels of deposition Choose one or combine into a single KDF?