## Slide 1
Exfoliation
Rice Husk
Commercial SiO2
Bio-SiO2
Egyptian Blue - nm
SiO2 extn
Characterisation
For each of the following processes, which variables will be changed? If yes, which?
EB synthesis – time and washing.
Exfoliation – power and pressure.
Spray Coating – which membranes?
Electrospinning – which polymers?
Process
Input/output
Characterisation
Legend
Input/output
Case Study 4.1 – Air Filters incorporating Egyptian Blue
SiO2
CaCO3
CuCO3.Cu(OH)3
H2O
Heating 32h
Egyptian Blue
32 h (3 kg)
Egyptian Blue 1 (500 g)
Egyptian Blue
32 h (500 g)
Egyptian Blue 2
(500 g)
Washing (HCl)
Heating 16h
Egyptian Blue
48 h (2kg)
Egyptian Blue
64 h (1kg)
Egyptian Blue 3 (500 g)
Egyptian Blue
48 h (500 g)
Egyptian Blue 4
(500 g)
Washing (HCl)
Heating 16h
Egyptian Blue 5 (500 g)
Egyptian Blue
64 h (500 g)
Egyptian Blue 6
(500 g)
Washing (HCl)
Characterisation
Characterisation
Characterisation
Characterisation
Characterisation
Characterisation
Characterisation
Characterisation
2 sources of SiO2
6 samples of EB – one of these selected for incorporation and/or conversion to nm form
Spray Coating
Electrospinning
Either source of SiO2 utilised in EB production according to the following scheme
The choice of incorporation method is to be determined by preliminary tests. Dip coating is the fallback option should electrospinning or spray coating not be feasible.
Input/output
Characterisation
Characterisation
Air Filter. Egyptian Blue - nm
Air Filter. Egyptian Blue - nm
Air Filter. Egyptian Blue - µm
Air Filter. Egyptian Blue - µm
Electrospinning
Air Filter. Egyptian Blue - nm
Air Filter. Egyptian Blue - nm
Air Filter. Egyptian Blue - µm
Air Filter. Egyptian Blue - µm
Spray Coating
Incorporation Step
The different colours for the products represents that Bio-SiO2 or commercial SiO2 could be utilised in the synthesis of EB
KDFs:
heating time (32, 48, 64 h);
washing step (yes,no).
Key Decision Factors