## Slide 1
Meeting
14/05/2025
MULTIDIMENSIONAL INTEGRATED QUANTITATIVE APPROACH TO ASSESS SAFETY AND SUSTAINABILITY OF NANOMATERIALS IN REAL CASE LIFE CYCLE SCENARIOS USING NANOSPECIFIC IMPACT CATEGORIES
This project has received funding from the European Union’s Horizon Europe research and innovation programme under GA No 101138414
STEFANO CERVELLERA

## Slide 2
INTEGRANO project – GA No: 101138414
Perovskites
AB
Sr
Inclusion of
Bio-Silica
KDF 1 - pH
KDF 2 – Red:Ox
0
1
1
0
NP4
NP5
NP6
NP7
O
Fe / Ce

## Slide 3
INTEGRANO project – GA No: 101138414
Characterization
Graphs report mean and standard deviation from three independent experiments

## Slide 4
INTEGRANO project – GA No: 101138414
Cell Viability
Graphs report mean and standard deviation from three independent experiments

## Slide 5
INTEGRANO project – GA No: 101138414
Cell Viability – why such differences
PARAMETER | NP4 (mean + sd) | NP5 (mean + sd)
DLS in MEDIUM t=0 100 ug/ml | 1565,22 ± 445,98 | 613,39 ± 122,74
DLS in MEDIUM t=24 100 ug/ml | 181,58 ± 13,62 | 196,34 ± 10,84
DLS in MEDIUM t=0 10 ug/ml | 1013,58 ± 434,84 | 593,48 ± 185,53
DLS in MEDIUM t=24 10 ug/ml | 192,55 ± 9,95 | 191,73 ± 9,99
Z-pot t=0 MQ | -23,26 ± 3,04 | -23,67 ± 2,47
KDF 1 – pH
KDF 2 – Red:Ox
0
1
1
0
NP4
NP5
NP6
NP7
=
Cell viability
=
=

## Slide 6
INTEGRANO project – GA No: 101138414
Cell Viability
Graphs report mean and standard deviation from three independent experiments

## Slide 7
INTEGRANO project – GA No: 101138414
Cell Viability – why such differences
PARAMETER | NP6 (mean + sd) | NP7 (mean + sd)
DLS in MEDIUM t=0 100 ug/ml | 979,12 ± 363,84 | 975,38 ± 204,88
DLS in MEDIUM t=24 100 ug/ml | 177,59 ± 6,32 | 188,5 ± 5,85
DLS in MEDIUM t=0 10 ug/ml | 1396,33 ± 213,29 | 1830,36 ± 178,85
DLS in MEDIUM t=24 10 ug/ml | 185,03 ± 3,21 | 186,71 ± 6,82
Z-pot t0 MQ | -17,42 ± 4,56 | -20,55 ± 4,28
KDF 1 – pH
KDF 2 – Red:Ox
0
1
1
0
NP4
NP5
NP6
NP7
=
Cell viability
=
=

## Slide 8
INTEGRANO project – GA No: 101138414
INFLAMMATION
Graphs report mean and standard deviation from three independent experiments

## Slide 9
INTEGRANO project – GA No: 101138414
INFLAMMATION
Graphs report mean and standard deviation from three independent experiments

## Slide 10
INTEGRANO project – GA No: 101138414
In the coming months
H2DCFDA
DNA damage
yH2AX Ab
Oxidative stress
Endpoints
Assays